Getzner Werkstoffe GmbH
Herrenau 5
6706 Bürs
Österreich

Tel. +43-5552-201-0
Fax +43-5552-201-1999
info.buers@getzner.com
www.getzner.com

Tender specifications

Impact sound insulation Getzner Stair Bearing SB10

| 1 | m | Getzner Stair Bearing SB10 Levelled surface free of heavy dirt. Remove outstanding stones and concrete edges. Delivering and installation of Stair Bearing according to manufacturer instructions. Stair Bearing out of Polyurethane-Elastomer and Polyethylene Filling Material, volume-compressible and free of softeners Product: Getzner Stair Bearing Type: SB10 or equal Thickness: 12 mm Form of delivery: 1500 mm Max. design load VRd: 75 kN/m Max. design load HRd: 5 kN/m Impact noise reduction ΔLw: 31 dB Flammability: Class E Required quantities for this project: SB10 S ______________________________ lfm SB10 I ______________________________ lfm SB10 L ______________________________ lfm SB10 Z ______________________________ lfm Joints must be sealed with duct tape to reduce structure borne noise bridges. An impact noise approval by an external expert acc. to DIN 7396 has to be submitted by the manufacturer if a different product has been suggested. Location of installation: _______________________________ | EUR/lfm EUR/lfm EUR/lfm Tender specification Getzner Stair Bearing SB10 en © by Getzner Werkstoffe GmbH ¦ 02-2015 EUR/lfm |
| --- | --- | --- | --- |
|  |  | Sum EUR: |  |